# TECHNICAL BULLETIN

GRAFFITI RESISTANCE

Canyon Tone Stain offers excellent coverage over graffiti stains; in most cases a single coat of Canyon Tone Stain will completely cover most graffiti related materials.

A coat of United Coating’s Arcysheen can also be added to Canyon Tone Stain applications to aid in the removal of graffiti stains.  Recommended coverage rate for Acrysheen used for this purpose is 100-150 square feet per gallon.

When tested in accordance with ASTM D-6578-00 Section 9 both spray paint and ink marker were easily removed from Canyon Tone Stain/Acrysheen applications with no noticeable change in sheen or appearance of coating system using Keton based cleaning solvents (M.E.K, Lacquer Thinner and most commercially available graffiti cleaning materials)

| Staining Agent | Cleaning Solution | Result | Finish Condition |
| --- | --- | --- | --- |
| Spray Paint (Red) | M.E.K Solvent | ## Stain was removed | Finish was retained |
| Spray Paint (Red) | M.E.K Solvent | Stain was removed | Finish was retained |
| Ink Marker (Blue) | Lacquer Thinner | Stain was removed | Finish was retained |
| Ink Marker (Blue) | Lacquer Thinner | Stain was removed | Finish was retained |

Successful removal of graffiti stains will vary greatly depending on type of graffiti material used, time that passes prior to cleaning and number of times graffiti is removed.

All small test area in a inconspicuous area is always recommend to test the suitability of cleaning solvent and method of removal.

www.canyontonestain.com