03/08/06

### File #: SF0649

Project:

Aquathon 150 Dirt Pick Up Resistance

Purpose:

To Determine “Dirt Pick-Up” Resistance (DPR) of Aquathon 150

Products:

Aquathon 150

Procedures:

- Prepare draw downs on ridged polypropylene

- Allow samples to cure for 24 hrs

- Expose half of sample to UV box (6 hrs) while protecting the other half with foil

- Expose entire sample to 80°C temperature for 1 week

- Run Urban DPR test (UCTM 002-05) by dry brushing and then washing with UCC

- Calculate DPR using X-rite L* value

Key Results:

| Product | L* |  | L* Yellowing Factored Out | Percent Whiteness Retained |  |
| --- | --- | --- | --- | --- | --- |
|  | UV Box (6Hrs) | Oven (80 C) | UV Box (6Hrs) | UV Box (6Hrs) | Oven (80 C) |
| 2 coats 150 BC, 1 coat 150 TC | 86.7 | 82.9 | 87.3 | 93.3% | 88.6% |
| 1 coat 150 BC, 1 coat 150 TC | 86.6 | 83.5 | 86.6 | 92.5% | 89.2% |
| 2 coats 150 TC | 93.0 | 93.6 |  |  |  |

Prepared by:

| Mike Mulgrew |  |
| --- | --- |
| Testing Technician |  |
| mulgrew@unitedcoatings.com |  |
| (509) 926-7143 ext. 151 |  |