# MAINTENANCE GUIDE

Although Canyon Tone Stain is designed for long-term service with little or no maintenance the following are recommended methods for extending the usable service of the product.

Specification:  When specifying Canyon Tone Stain, consider the type of color to be used.  Earth tone and medium based colors are the longest lasting and require the least amount of maintenance. Consider limiting bright or intense colors to bands or accent details of the design, as these types of colors will have a certain amount color shift over time due to oxidation of the colorant system used.  When large areas of intense colors are needed, it is recommended that these areas be topcoated with a clear sealer, such as United Coatings’ Acrysheen, to prevent the colorants from oxidizing.

Maintenance:  In most cases rain will sufficiently remove most common pollutants from Canyon Tone Stain.  If cleaning is required, use a biodegradable cleaner such as United Coatings’ UCC Cleaner and a soft bristle brush or light duty power wash to remove pollutants.  If mold or mildew is present, pre-treat effect areas with a solution of 1-quart house hold bleach and 5 quarts warm water.  Allow solution to saturate the effected area and clean with UCC Cleaner.

Graffiti Stains:  Canyon Tone Stain provides excellent coverage over most graffiti stains.  If a graffiti-resistant product is required, specify or apply one coat of United Coatings Acrysheen sealer.  Graffiti can then be removed using any commercially available graffiti removal solvent.   Note: some temporary softening of the Acrysheen is normal when solvents are used for removal.

Re-application:  If recoating of Canyon Tone Stain is required, clean the area to be recoated as outline in the “Maintenance” paragraph above.  Apply one coat of Canyon Tone Stain to a small test area to determine if a single coat will provide an acceptable finish.  Apply Canyon Tone Stain in strict accordance with published literature.  Recommended recoat application rate is 200 square feet per gallon per coat.  Note:  While Canyon Tone Stain is on excellent choice for recoating itself, it is not recommended as a recoat product for other coating systems.

www.canyontonestain.com