TECHNICAL BULLETIN

# CANYON TONE STAIN OVER HORIZONTAL SURFACES

From time to time, Canyon Tone Stain is used on a horizontal application subject to pedestrian or light vehicular traffic.  These applications include walkways, patios, pool decks, floors, balconies, lanais, driveways and entryways.  When applied properly, Canyon Tone Stain can provide an effective color-coat over these areas.

As with any application, surface preparation is critical.  The surface must be clean and dry, and be free from oil, grease, dirt, curing compounds, latence and any other contamination that may prevent proper adhesion.  The Canyon Tone Stain must be able to penetrate the surface to be effective, therefore, existing paints or coatings must be completely removed.  Steel trowelled floors or other dense surfaces must be blasted or thoroughly acid-etched to “open up” the surface and allow the stain to penetrate.  Care must be taken on any repair work to match the finish texture of the repaired area to the surrounding concrete.  As Canyon Tone Stain is designed to preserve the natural texture of the substrate, any variances in the finish will be reflected once the stain is applied.

Canyon Tone Stain can be applied by roller or airless spray over horizontal surfaces, however, if airless spray is utilized, the first coat should be back-rolled to work the stain into the pores of the concrete.  Canyon Tone should be applied in two thin coats, at the rate of 300 to 400 square feet per gallon per coat.  A heavier film is not better, and will only increase the potential for peeling.  The first coat should also be thinned approximately 20 to 25% with water to maximize the penetration.  Allow adequate dry time prior to subjecting the coated surfaces to any traffic.

Service life is a function of how much wear the surface receives.  Canyon Tone Stain applied over horizontal surfaces should be considered a “maintenance” application.  It will wear, particularly on the high points, and will require touchup or recoating as it wears.  Properly applied, Canyon Tone Stain will provide an attractive, functional color coat over horizontal concrete surfaces.  A topcoat of Acrysheen will help to provide additional wear resistance and ease of cleanability.  Due to the critical importance of surface preparation and the variables associated with the amount of traffic the surface will receive, UNITED offers no warranties or guarantees for Canyon Tone Stain used on horizontal applications.