June 22, 1998

# Test Report

Canyon Tone Stain (CTS) and 1996 FHWA Standard Specification Book Requirements.

Our water-based CTS meets and/or exceeds the following standards:

| Property | Requirement | Typical value for CTS |
| --- | --- | --- |
| Mildew Resistance, as per Federal Test Method 244, Method 6271 | Pass | Pass as per ASTM G21, which is equivalent to FTM 244, Method 6271. CT\S will pass any bio-resistance standard from the Singapore Protocol to ASTM. 2,3 |
| Accelerated Weathering, as per ASTM G-53 @ 1000 hours | Pass | Pass at 2,000 hours for both color stability and chalking. 1 |
| Acrylic Content: Acrylic Dispersion as a percentage of non-volatile vehicle | >73.4% | 88.2% 5 |
| Viscosity | 58 +/- 2 KU | 58 KU 4 |
| Solids Content | >40.3% | 42.5% 5 |

Steve Heinje

Technical Director

Sources:

- Canyon Tone Benchmark Study 1997

- Bioefficacy Evaluations…, Rohm and Haas August 13th, 1991

- Microbiology Laboratory Report M97-159, April 21,1997

- Don Lilly,  Quality Control

- ASTM 5201 with Batch Master Software