| #### Certificate of Analysis |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Water Absorption |  |  |  |  |  |  |  |  |  |  |
| Product Name |  | Elastuff 120 |  |  |  |  |  |  |  |  |
| Batch Number |  | Part A: 99229, Part B: 99230 |  |  |  |  |  |  |  |  |
| Manufacture Date |  | 05 May 05 |  |  |  |  |  |  |  |  |
| Test Date |  | 19 Feb 07 |  |  |  |  |  |  |  |  |
| Application/Date |  | 10 March 06 / 160o F. material temperature at 3000 psi pump pressure |  |  |  |  |  |  |  |  |
| Test Method |  | ASTM D-570 Water Absorption of Plastics |  |  |  |  |  |  |  |  |
| Test Conditions |  | As per ASTM standard. Any deviation reported at end of certificate. |  |  |  |  |  |  |  |  |
| This certificate confirms that the above product was tested as per stated standard |  |  |  |  |  |  |  |  |  |  |
| specification using calibrated equipment and qualified staff. The following test results |  |  |  |  |  |  |  |  |  |  |
| were obtained. |  |  |  |  |  |  |  |  |  |  |
| Test Results |  |  |  |  |  |  |  |  |  |  |
| Parameter |  |  |  |  |  |  |  | % Wt Gain |  |  |
| Sample A |  |  |  |  |  |  |  | 0.8700 |  |  |
| Sample B |  |  |  |  |  |  |  | 0.778 |  |  |
| Sample C |  |  |  |  |  |  |  | 0.8187 |  |  |
| Average Gain |  |  |  |  |  |  |  | 0.8222 |  |  |
| Test conditions (if different from standard test conditions) and/or notes. |  |  |  |  |  |  |  |  |  |  |
| Test Temperature 26°C |  |  |  |  |  |  |  |  |  |  |

Prepared by:

| Mike Sand |  |
| --- | --- |
| Research Lab Manager |  |
| mike@unitedcoatings.com |  |
| (509) 688-2335 |  |