12-19-03

### File #: CS 0741

Project:

Elastuff 120 Physical Properties Testing

Purpose:

Summarize the following test results for Elastuff 120: Adhesion to Concrete, Crack Bridging Ability, Accelerated Weathering, Softening Point & Salt Spray Resistance.

Products:

Elastuff 120 applied to concrete and steel panels, depending on the test.

Procedures:

Elastuff 120 parts A and B were mixed according to product specifications then applied to concrete and steel panels.  After allowing to cure for a minimum of 7 days, the following test results were obtained:

Results:

— Test Results —

|  | #### Test Method | Result |
| --- | --- | --- |
| Elcometer Adhesion | ASTM D4541 | >350 psi over Concrete |
| Crack Bridging Ability | ASTM C1305 | No Cracking or Fatigue |
| Accelerated Weathering | ASTM G154 QUV Cabinet | 5,000 Hours |
| Softening Point | ASTM D36 | >325 degrees F |
| Salt Spray Resistance | ASTM B117 | No Adverse Effects |

Discussion or Conclusion:

Elastuff 120 meets or exceeds all requirements for the specified application.

Prepared by:

Mike Sand

Lead Chemist

mike@unitedcoatings.com

(509) 926-7143 ext. 135