| Certificate of Analysis |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Tensile Strength |  |  |  |  |  |  |  |
| Product Name |  | Uniflex 255 |  |  |  |  |  |
| Batch Number |  | Part A: 65805, Part B: 66388 |  |  |  |  |  |
| Test Date |  | 12-1988 |  |  |  |  |  |
| Test Method |  | ASTM D-412 Vulcanized Rubber & Thermoplastic Elastomers |  |  |  |  |  |
| Test Conditions |  | As per ASTM standard. Any deviation reported at end of certificate. |  |  |  |  |  |
| This certificate confirms that the above product was tested as per stated standard |  |  |  |  |  |  |  |
| specification using calibrated equipment and qualified staff. The following test results |  |  |  |  |  |  |  |
| were obtained. |  |  |  |  |  |  |  |
| Test Results |  |  |  |  |  |  |  |
| Parameter |  |  |  |  | Symbol | Unit | Result |
| Tensile Strength |  |  |  |  | TS | MPa | 21 |
|  |  |  |  |  |  | PSI | 3045 |
| Elongation |  |  |  |  | E | % | 166% |
| Test conditions (if different from standard test conditions) and/or notes. |  |  |  |  |  |  |  |
| Test Equipment: Instron Physical Properties Tester |  |  |  |  |  |  |  |
| Temperature and Humidity: 23oC / 24% RH. |  |  |  |  |  |  |  |
| Roseann Kilbane |  |  |  |  |  |  |  |
| Testing Technician |  |  |  |  |  |  |  |
| United Caotings |  |  |  |  |  |  |  |