# Elastuff 200

Reference 10R423/24

06-18-2003

Physical Properties

| Property | Test Method | Part A | Part B |
| --- | --- | --- | --- |
| Color |  |  |  |
| Viscosity cps | ASTM D-2196 | 500-1000 | 500 - 1000 |
| Solids % |  | 100 | 100 |
| Density pounds/gallon | ASTM D1475 | 7.88 | 7.62 |
| Shelf Life |  | 12 months | 12 months |

Performance Properties

| Property | Test Method | Result |
| --- | --- | --- |
| Gel time |  | 10 Seconds |
| Tack Free Time |  | 5 Minutes |
| Full cure |  | 24 Hours |
| Adhesion | ASTM D-4541 |  |
| Concrete |  | >900 psi(6.2 kPa)1,4 |
| Steel |  | >1300psi(8.9 kPa)2,3 |
| Tensile Strength | ASTM D-412 | 2700psi(18.6 kPa) |
| Elongation | ASTM D-412 | 550% |
| Tear Strength | ASTM D-624 | 425 pli(74.5 Kn/m) |
| Hardness Shore A/D | ASTM D-2240 | 90/45 |
| Perms | ASTM D-1653 | 0.2 |
| Taber Abrasion CS-17 1000 cycles | ASTM D-4060 | 0.6 mg loss |

1 Primed with Unitile Sealer

2 Although exelent adhesion values were obtained,  to insure proper adhesion and wetting it is

recommended the surface be primed with Primer 302 prior to Elastuff 200 application.

3 Coating cohesive failure

4 Concrete cohesive failure