# Elastuff 300

Reference 10R401

06-18-2003

#### Physical Properties

| Property | Test Method | Part A | Part B |
| --- | --- | --- | --- |
| Color |  |  |  |
| Viscosity cps | ASTM D-2196 | 1000 - 2000 | 500 - 1000 |
| Solids % |  | 100 | 100 |
| Density pounds/gallon | ASTM D1475 | 9.35 | 8.59 |
| Shelf Life |  | 12 months | 12 months |

#### Performance Properties

| Property | Test Method | Result |
| --- | --- | --- |
| Gel time |  | 10 Seconds |
| Tack Free Time |  | <5 Minutes |
| Full cure |  | 24 Hours |
| Adhesion | ASTM D-4541 |  |
| Concrete |  | 1100psi (7.6 kPa)1,2 |
| Steel |  | 1700psi (11.75 kPa)3 |
| Tensile Strength psi | ASTM D-412 | 3500 psi (24 kPa) |
| Elongation | ASTM D-412 | 310% |
| Tear Strength | ASTM D-624 | 480 pli(81 kN/m) |
| Hardness Shore A/D | ASTM D-2240 | 95/55 |
| Perms | ASTM D-1653 | 0.2 |
| Taber Abrasion CS-17 1000 cycles | ASTM D-4060 | 1.2 mg loss |

1 Substrate Cohesive failure

2 Primed with Unitile Sealer

3 Although exelent adhesion values were obtained,  to insure proper adhesion and wetting it is

recommended the surface be primed with Primer 302 prior to Elastuff 300 application.