01/19/05

### File #: SF 0586

#### ELASTUFF 110 ADVANTAGES

Elastuff 110 is based on advanced, 100% solids rigid polyurethane technology. The Part A and Part B resins are based on multifunctional polymers containing three to four reactive groups each. When reacted, they form a dense, three-dimensional, highly cross-linked structure.  The bonding forces within this structure are much greater than those present between polymer chains in typical polyurethane elastomer coatings, which are based mainly on difunctional resins.  As a result, Elastuff 110 offers improved coating properties including increased hardness, tensile strength, cohesive strength and modulus, and adhesion, as well as superior chemical resistance with reduced solubility.

The following chart shows the effects of various hydrocarbon materials on Elastuff 110 when tested as per ASTM D-1308 after 7-day exposure.

| Solvent |  |  | Result |
| --- | --- | --- | --- |
| Gasoline |  |  | No effect |
| Oil |  |  | No effect |
| Diesel |  |  | No effect |
| Jet fuel (JP-4) |  |  | No effect |
| ## Anti-freeze |  |  | No effect |
| Automatic Transmission Fluid |  |  | No effect |
| Brake Fluid |  |  | Slight swelling / slight softening |
| Xylene |  |  | No effect |
| Hexane |  |  | No effect |
| Ethanol |  |  | No effect |
| Grease |  |  | No effect |
| Power Steering Fluid |  |  | No effect |
| Lighter Fluid |  |  | No Swelling/Modest discoloration |
| Graphite Lube |  |  | No effect |
| Paint Thinner |  |  | No effect |

## UNITED COATINGS

## Mike Sand

## Chemist