# Elastuff 310

Reference 10R402

03-11-2003

Physical Properties

| Property | Test Method | Part A | Part B |
| --- | --- | --- | --- |
| Color |  |  |  |
| Viscosity cps | ASTM D-2196 | 1000 - 2000 | 500 - 1000 |
| Solids % |  | 100 | 100 |
| Density pounds/gallon | ASTM D1475 | 9.35 | 8.59 |
| Shelf Life |  | 12 months | 12 months |

Performance Properties

| Property | Test Method | Result |
| --- | --- | --- |
| Gel time |  | 10 Seconds |
| Tack Free Time |  | 5 Minutes |
| Full cure |  | 24 Hours |
| Adhesion | ASTM D-4541 |  |
| Concrete |  | 900 psi(6.2 kPa)1,2 |
| Steel |  | 1100psi(7.6 kPa)1,3 |
| Tensile Strength | ASTM D-412 | 2200psi(15.2 kPa) |
| Elongation | ASTM D-412 | 280% |
| Tear Strength | ASTM D-624 | 420 pli(73.5 kN/m) |
| Hardness Shore A/D | ASTM D-2240 | 95/50 |
| Perms | ASTM D-1653 |  |
| Taber Abrasion CS-17 1000 cycles | ASTM D-4060 | 0.6 mg loss |

1 Actual adhesion is higher as failure occurred within the epoxy adhesive/loading fixture interface.

Coating remained 100% adhered to surface.

2 Primed with Unitile Sealer.

3 Although excellent adhesion values were obtained, to insure proper adhesion and wetting it is

recommended the surface be primed with Primer 302 prior to Elastuff 310 application.